P14	AIR/WIND TIGHTNESS VAPOUR PERMEABLE LAYERS

To be read with the Preliminaries A10-A55 /General Conditions and A90 & A94.

PRODUCTS

322A	GUN APPLIED ADHESIVE TO POROUS STRUCTURAL SURFACES:

Manufacturer: MOLL bauökologische Produkte GmbH, See P14/509K

Product Reference: Orcon F

Importing Agents: Ecological Building Systems See P14/509K

Adhesive: tubular film sleeve or cartridge for use with standard applicator gun,

Material:

Non-ageing Acrylate polymers without softeners or halogenated compounds which is insusceptible to embrittlement.

Contains denatured alcohol (15%) allowing it to penetrate deep into stone substrates, ensuring a very tight bond.

Properties:

Exceptionally high inner strength (cohesion) while also being elastic.

Outstanding adhesion to building materials gives the joint the necessary safety and longevity.

High strength on building material substrates

Greater resistance to high humidity on building sites

Long lasting adhesion and elasticity

Frost resistant: to -20° C

Temperature range: -20° C to +80° C

Low VOC: compliant with Sentinel House Institute German indoor Air Quality standard

Life expectancy: 60+ years

Airtight bonding to DIN 4108-7, SIA 180 and ONorm B8110-2

3rd party accreditation:

NSAI Agrément Certificate: NSAI 07/0297

Applications:

Internal and external

Airtight outdoor joints e.g. vapour check for external roof insulation

Airtight outdoor joints e.g. sub or top vapour check for refurbishment reroofing

Wind proof bonding of roof underlay

Wind proof bonding of façade membranes

Use with:

Pro clima Intello Plus to P14/310A

Pro clima DB+ to P14/311A

all of Pro clima’s vapour checks, air-tightness and wind-tightness membranes,

PE Polyethylene

PA Polyamide (Nylon)

PP polypropylene

aluminium foils

Product Page: http://www.greenspec.co.uk/html/product-pages/orconf.php

Use: Multipurpose joint adhesive

Suitable for bonding to following:

To smooth, rough or stony surfaces, to concrete, plaster, render, lime based mineral plasters.

Do not use on:

unstable or crumbling surface unless grounded and stabilised See P14/580B

unprotected metal surfaces.

Rust resistant metals: See Pro clima Duplex to P14/355A

Preparation:

Damp surfaces: allow to dry

Grounding and stabilising: to P14/580

Packaging: tubular film sleeve or cartridge for use with standard applicator gun,

Application rate:

310 ml (g) cartridge approx. 5-10 m.

600 ml refill tube for approx. 10-25 m.

Application:

Internal and external applications

smooth surfaces: 5 mm. thick continuous bead

Mineral or rough structural component surfaces: increase bead size as necessary.

Following trades: Does not require a pressure batten.

Delay between sealing and air testing: 12 to 24 hours depending on weather conditions

© 2000-2009 NGS GreenSpec

REV	REVISIONS

| Revision No | Description | Author | Date | Checked by |
| --- | --- | --- | --- | --- |
| A00 | For Preliminary Issue Extracted from Specification file A11 %%% | BRM | 14/12/2009 |  |
| B00 | Reviewed, post on Website |  |  |  |

Terms and Conditions

1 The ‘Information’

1.1 The ‘Green Building Specification’ is a service provided by GreenSpec.  These terms and conditions may be revised from time to time without prior notice.

1.2 This draft specification was prepared for the GreenSpec ‘Green Building Specification’ by Architectural Specification Writing Services (ASWS).

1.3 The specification clauses in this document (the 'Information') are based on past project work, information gathered from seminars, workshops and assimilated from published or unpublished verbal and written information.

1.4 The Information will continue to be developed and current files will be maintained on the GreenSpec website at www.greenspec.co.uk

2 Copyright Notice

2.1 Copyright and all other intellectual property rights in the Information shall remain at all times the property of GreenSpec and you shall acquire no rights in any such material except as expressly provided in this Agreement.

2.2 You are permitted to reproduce any part or parts either alone or in conjunction with your own material for the purposes of internal use in the your office, or for inclusion in any drawings or contract documents used or intended to be used in connection with a building contract where you are contracting party, or in connection with which you are engaged by one of the contracting parties in a professional capacity.

2.3 You shall not use, sell, assign, rent, sub-license, loan, or otherwise deal in any way in the Information or any interest in it except as expressly provided herein.

3 Disclaimer

3.1 Whilst GreenSpec endeavours to ensure that the Information is correct, it is provided on an "as is" basis, without warranties of any kind, and no warranty, express or implied, is given as to accuracy, currency or completeness and GreenSpec does not accept any liability for any error or omission.  GreenSpec shall not be liable for any third party claims or losses of any nature including, but not limited to, loss of profits, direct, indirect, special or consequential damages arising from a third party's use or inability to use this Information.

3.2 All users and others must verify the contents of the Information and ensure that its application is effective to communicate what is required by them and that the Information is fit for their intended use which has not been specified by GreenSpec.

3.3 GreenSpec accepts no responsibility for the content on any internet website to which a hypertext link from this specification exists.  The links are provided "as is" with no warranty, express or implied, for the information provided within them.

4 General

4.1 If any part of this Agreement is held by a court of competent jurisdiction to be unenforceable the validity of the remainder of the Agreement will not be affected.

4.2 This Agreement is covered by the Laws of England and Wales.

______________________________________________________]

Addenda

NBS compatibility

National Building Specification (NBS) is the industry standard specification library.

GreenSpec’s Green Building Specification (GBS) is designed to complement NBS.

GreenSpec clauses are written specifically to address issues of environmental sustainability.

NBS adopts and develops the Construction Project Information Committee’s (CPIC) classification system Common Arrangement of Work Sections (CAWS) 1998 edition.

GBS adopts and develops the CPIC and NBS versions of CAWS to enable integration into NBS-based specifications.

GBS adopts NBS clause numbering to provide for easy clause assimilation.

CPIC: www.productioninformation.org/

CAWS: www.productioninformation.org/CAWS.asp

Proposed changes: www.productioninformation.org/cawsuni/topcawsuni.asp

NBS: www.thenbs.com/