P14	AIR/WIND TIGHTNESS VAPOUR PERMEABLE LAYERS

To be read with the Preliminaries A10-A55 /General Conditions and A90 & A94.

PRODUCTS

311A	AIR TIGHT & HUMIDITY VARIABLE PERFORMANCE VAPOUR CHECK MEMBRANE:

System: Complete intelligent air-tightness system with all necessary adhesive agents.

Manufacturer: MOLL bauökologische Produkte GmbH, See P14/509K

Reference: Pro clima DB+,

Importing Agents: Ecological Building Systems See P14/509K

UK & Ireland Agent: Ecological Building Systems UK Ltd. See P14/509K

Product Page: http://www.greenspec.co.uk/html/product-pages/db_plus.php

3rd party Certification:

natureplus Certificate No.: 1701_0901_083_1 Valid until Jan 2012

NSAI Agrément Certificate: NSAI 07/0297

CE Mark in accordance with DIN EN 13984

Properties:

Breaking Load:

MD: 550 N/50mm

CD: 310 N/50mm

Durability: to EN 13984

Application:

Internal face only,

ecological and good indoor air quality projects,

Protection for thermal insulation systems against penetrating moisture, damage and mould.

Reduction in cold air penetration and hot air loss, reducing energy in use of the building and CO2 emissions.

Airtight and vapour permeable,

Reduces risk of interstitial condensation in summer and winter

Permits vapour to escape internally from constructions with vapour impermeable materials externally

Humidity-variable diffusion resistant membrane

Water Vapour Transmission Resistance:

sd: (Humidity variable) 0.60 m to 4 m (2.3 m)

Standard dew point assessment/calculation to BS EN 13788

Permeance: 5.4 to 0.82 US perms

MVTR: <3.06 to >20.4 MNs/g

Surface weight: 185 g/m2

Vapour diffusion resistance: 10 MNs/g at an average humidity of 60% (room 70%, construction 50%)

Fire class: E, treated with natural salts against fire

Temperature resistance: Long-lasting up to -40° C to + 80° C

Tear resistant due to reinforcement.

Environmental Credentials:

Country of origin and manufacture: Germany,

Diffusion Open product for use in breathing construction,

Natural content: cellulose fibre paper,

Recycled content: cellulose fibre paper 50 % to ISO 14021

Recyclable.

Material: natural and recycled cellulose fibre Kraftpaper, glued with a thin halogen-free and plasticiser-free PE Polyethylene film, plastic mesh reinforced for additional strength and treated with natural salts against fire

Thickness: 0.23 mm.

Roll size: 1350 mm. x 50 m. (standard size, others available subject to order, upon request)

Accreditation: CE Mark in accordance with DIN EN 13984

The membrane has no front and back side and can be fitted with either the printed or the unprinted side facing the room.

The printed markings are only an aid to orientation.

Use with the following sealing adhesive tapes and adhesives:

Adhesives:

Ecological and good indoor air quality Pro clima Eco Coll to P14/320A

Pro clima Orcon F to P14/322A

Adhesive tapes:

Unitape to P14/330A

Tescon No. 1 to P14/336A

© 2000-2009 NGS GreenSpec

REV	REVISIONS

| Revision No | Description | Author | Date | Checked by |
| --- | --- | --- | --- | --- |
| A00 | For Preliminary Issue Extracted from Specification file A11 %%% | BRM | 14/12/2009 |  |
| B00 | Reviewed, post on Website |  |  |  |

Terms and Conditions

1 The ‘Information’

1.1 The ‘Green Building Specification’ is a service provided by GreenSpec.  These terms and conditions may be revised from time to time without prior notice.

1.2 This draft specification was prepared for the GreenSpec ‘Green Building Specification’ by Architectural Specification Writing Services (ASWS).

1.3 The specification clauses in this document (the 'Information') are based on past project work, information gathered from seminars, workshops and assimilated from published or unpublished verbal and written information.

1.4 The Information will continue to be developed and current files will be maintained on the GreenSpec website at www.greenspec.co.uk

2 Copyright Notice

2.1 Copyright and all other intellectual property rights in the Information shall remain at all times the property of GreenSpec and you shall acquire no rights in any such material except as expressly provided in this Agreement.

2.2 You are permitted to reproduce any part or parts either alone or in conjunction with your own material for the purposes of internal use in the your office, or for inclusion in any drawings or contract documents used or intended to be used in connection with a building contract where you are contracting party, or in connection with which you are engaged by one of the contracting parties in a professional capacity.

2.3 You shall not use, sell, assign, rent, sub-license, loan, or otherwise deal in any way in the Information or any interest in it except as expressly provided herein.

3 Disclaimer

3.1 Whilst GreenSpec endeavours to ensure that the Information is correct, it is provided on an "as is" basis, without warranties of any kind, and no warranty, express or implied, is given as to accuracy, currency or completeness and GreenSpec does not accept any liability for any error or omission.  GreenSpec shall not be liable for any third party claims or losses of any nature including, but not limited to, loss of profits, direct, indirect, special or consequential damages arising from a third party's use or inability to use this Information.

3.2 All users and others must verify the contents of the Information and ensure that its application is effective to communicate what is required by them and that the Information is fit for their intended use which has not been specified by GreenSpec.

3.3 GreenSpec accepts no responsibility for the content on any internet website to which a hypertext link from this specification exists.  The links are provided "as is" with no warranty, express or implied, for the information provided within them.

4 General

4.1 If any part of this Agreement is held by a court of competent jurisdiction to be unenforceable the validity of the remainder of the Agreement will not be affected.

4.2 This Agreement is covered by the Laws of England and Wales.

______________________________________________________]

Addenda

NBS compatibility

National Building Specification (NBS) is the industry standard specification library.

GreenSpec’s Green Building Specification (GBS) is designed to complement NBS.

GreenSpec clauses are written specifically to address issues of environmental sustainability.

NBS adopts and develops the Construction Project Information Committee’s (CPIC) classification system Common Arrangement of Work Sections (CAWS) 1998 edition.

GBS adopts and develops the CPIC and NBS versions of CAWS to enable integration into NBS-based specifications.

GBS adopts NBS clause numbering to provide for easy clause assimilation.

CPIC: www.productioninformation.org/

CAWS: www.productioninformation.org/CAWS.asp

Proposed changes: www.productioninformation.org/cawsuni/topcawsuni.asp

NBS: www.thenbs.com/