P14	AIR/WIND TIGHTNESS VAPOUR PERMEABLE LAYERS

To be read with the Preliminaries A10-A55 /General Conditions and A90 & A94.

PRODUCTS

317A	WIND TIGHT, VAPOUR PERMEABLE, PITCHED ROOF UNDERLAY:

System: Complete vapour permeable wind-tightness system with all necessary adhesive agents.

Manufacturer: MOLL bauökologische Produkte GmbH, See P14/509K

Reference: Pro clima Solitex Plus

Accreditation: CE Mark in accordance with DIN EN 13984

British Board of Agrément Certificate: BBA 07/4432 Pro clima Solitex Vapour permeable roofing underlay

Irish Agrément Certificate:

IBA 02/0138 Solitex Plus & Solitex UD Vapour Permeable Roofing Underlays for Pitched Roofs

NSAI Agrément Certificate: NSAI 07/0297

3rd party product endorsement: NHBC Standards 2007

Importing Agents: Ecological Building Systems See P14/509K

Product page: http://www.greenspec.co.uk/html/product-pages/solitex_plus.php

Applications:

External only

unsupported and supported tiled or slated pitched roof underlay

warm ventilated and non-ventilated tiled or slated pitched roofs

cold ventilated and non-ventilated tiled or slated pitched roofs.

Materials: 4 layers

Roof tile underlay with net reinforcement.

Outer layers: spun bonded polypropylene felt fabric

central layer: monolithic nonporous TEEE (thermoplastic ether ester elastomer) membrane

reinforcement net: Polypropylene

Manufacturing process: bonding together through an extrusion-coating process, using a combination of heat and pressure in a continuous process.

Performance:

provides a barrier to minimise the effects of wind load generated under wind gusts acting on slates and tiles when installed in accordance with this Certificate.

facilitate the control of surface and interstitial condensation in insulated roofs.

roof tile underlay offers resistance to tearing during installation and will give higher flexibility at low ambient temperatures.

Properties:

sd value: 0.03m or < than 0.15MNs/g See table in BBA Certificate.

Water vapour resistance: < 0.15 MNs/g

Nail tear resistance: > 350 N/m

Waterproof: > 2500 mm. of water column, waterproof when subjected to heavy rain.

Wind driven pelting rain: extreme resistance

Temperature range: -40 degrees C to +100 degrees C

Weight: 170 g/m2

Fire Rating E

Standard: Exceeds Type 1F reinforced bitumen underlay to BS 747

Roll size: 1500 mm. x 50 m. (smaller rolls available for window and floor connections)

Colour: Mid Blue & Dark blue text stripe/Dark grey & white grid back

Environmental Credentials:

Country of origin and manufacture: Germany,

Attributes:

Diffusion Open product for use in air impermeable moisture breathing construction,

Site issues:

Can be exposed to the elements for 6 months.

It must only be fitted using staples or tacks in areas protected by an overlap.

To maximise the windtightness of the external membrane It is imperative that all taping and attachment is done with utmost care.

Ensure detailed planning, particularly of fitting at the eaves and gables,

Ensure careful execution when fitting insulation over rafters.

Small damage repairs: Pro clima Tescon No. 1: to P14/332A

Services apertures: Pipe Grommet: Pro clima Roflex to P14/343A or P14/344A

Delay between taping/sealing and air testing: Generally: 10 minutes minimum.

© 2000-2009 NGS GreenSpec

REV	REVISIONS

| Revision No | Description | Author | Date | Checked by |
| --- | --- | --- | --- | --- |
| A00 | For Preliminary Issue Extracted from Specification file A11 %%% | BRM | 14/12/2009 |  |
| B00 | Reviewed, post on Website |  |  |  |

Terms and Conditions

1 The ‘Information’

1.1 The ‘Green Building Specification’ is a service provided by GreenSpec.  These terms and conditions may be revised from time to time without prior notice.

1.2 This draft specification was prepared for the GreenSpec ‘Green Building Specification’ by Architectural Specification Writing Services (ASWS).

1.3 The specification clauses in this document (the 'Information') are based on past project work, information gathered from seminars, workshops and assimilated from published or unpublished verbal and written information.

1.4 The Information will continue to be developed and current files will be maintained on the GreenSpec website at www.greenspec.co.uk

2 Copyright Notice

2.1 Copyright and all other intellectual property rights in the Information shall remain at all times the property of GreenSpec and you shall acquire no rights in any such material except as expressly provided in this Agreement.

2.2 You are permitted to reproduce any part or parts either alone or in conjunction with your own material for the purposes of internal use in the your office, or for inclusion in any drawings or contract documents used or intended to be used in connection with a building contract where you are contracting party, or in connection with which you are engaged by one of the contracting parties in a professional capacity.

2.3 You shall not use, sell, assign, rent, sub-license, loan, or otherwise deal in any way in the Information or any interest in it except as expressly provided herein.

3 Disclaimer

3.1 Whilst GreenSpec endeavours to ensure that the Information is correct, it is provided on an "as is" basis, without warranties of any kind, and no warranty, express or implied, is given as to accuracy, currency or completeness and GreenSpec does not accept any liability for any error or omission.  GreenSpec shall not be liable for any third party claims or losses of any nature including, but not limited to, loss of profits, direct, indirect, special or consequential damages arising from a third party's use or inability to use this Information.

3.2 All users and others must verify the contents of the Information and ensure that its application is effective to communicate what is required by them and that the Information is fit for their intended use which has not been specified by GreenSpec.

3.3 GreenSpec accepts no responsibility for the content on any internet website to which a hypertext link from this specification exists.  The links are provided "as is" with no warranty, express or implied, for the information provided within them.

4 General

4.1 If any part of this Agreement is held by a court of competent jurisdiction to be unenforceable the validity of the remainder of the Agreement will not be affected.

4.2 This Agreement is covered by the Laws of England and Wales.

______________________________________________________]

Addenda

NBS compatibility

National Building Specification (NBS) is the industry standard specification library.

GreenSpec’s Green Building Specification (GBS) is designed to complement NBS.

GreenSpec clauses are written specifically to address issues of environmental sustainability.

NBS adopts and develops the Construction Project Information Committee’s (CPIC) classification system Common Arrangement of Work Sections (CAWS) 1998 edition.

GBS adopts and develops the CPIC and NBS versions of CAWS to enable integration into NBS-based specifications.

GBS adopts NBS clause numbering to provide for easy clause assimilation.

CPIC: www.productioninformation.org/

CAWS: www.productioninformation.org/CAWS.asp

Proposed changes: www.productioninformation.org/cawsuni/topcawsuni.asp

NBS: www.thenbs.com/