P14	AIR/WIND TIGHTNESS VAPOUR PERMEABLE LAYERS

To be read with the Preliminaries A10-A55/General Conditions and A90 & A94.

PRODUCTS

370B	PRIMER/STABILISER

Manufacturer: MOLL bauökologische Produkte GmbH, See P14/509K

Product Reference: Pro clima Tescon Primer RP.

Importing Agents: Ecological Building Systems See P14/509K

Applications: Floors, Roofs, Walls, structure,

Suitable backgrounds:

Plastered surfaces

Wood fibreboard surfaces

Woodfibreboard softboard to P10/___ e.g. Gutex

Wood

Blockwork walls

Concrete

Sand cement screed

Plaster skimmed surfaces

Use with and prepare surface for:

Adhesives:

Ecological and good indoor air quality Pro clima Eco Coll to P14/320A

Pro clima Orcon F to P14/322A

Adhesive tapes:

Pro clima Tescon No. 1 to P14/332A

Pro clima Tescon Vana to P14/332B

Pro clima Tescon Profil to P14/336A

Material: Solvent-free Acrylate copolymer primer

Dissolvent: water

Properties:

Working temperature: +2 to +45 degrees C

Temperature resistance: -40 to +90 degrees C

Storage: frost protection, frost-free, shelf life 24 months

Contents: 0.75, 1 or 2.5 litres

Coverage: 7.5 m2, 10 m2 or 25 m2

Mixing: shape bottle before application,

Preparation: surfaces shall be:

Free from dust, loose materials, or sawdust

Smooth, dry and stable

Surfaces may be wet, bond will still be achievable

Thawed and not frozen

Surfaces must be set and fully cured and dried

Application: to P14/580A

For speedy application: no drying of primer is necessary

Bonding of Tescon No.1 to P14/332A or Tescon Vana to P14/332B to wet primer is possible

Use with wind tightness underlay membranes:

Pro clima Solitex Plus: to P14/317A

Pro clima Intello Plus to P14/310A

© 2000-2009 NGS GreenSpec

REV	REVISIONS

| Revision No | Description | Author | Date | Checked by |
| --- | --- | --- | --- | --- |
| A00 | For Preliminary Issue Extracted from Specification file A11 %%% | BRM | 14/12/2009 |  |
| B00 | Reviewed, post on Website |  |  |  |

Terms and Conditions

1 The ‘Information’

1.1 The ‘Green Building Specification’ is a service provided by GreenSpec.  These terms and conditions may be revised from time to time without prior notice.

1.2 This draft specification was prepared for the GreenSpec ‘Green Building Specification’ by Architectural Specification Writing Services (ASWS).

1.3 The specification clauses in this document (the 'Information') are based on past project work, information gathered from seminars, workshops and assimilated from published or unpublished verbal and written information.

1.4 The Information will continue to be developed and current files will be maintained on the GreenSpec website at www.greenspec.co.uk

2 Copyright Notice

2.1 Copyright and all other intellectual property rights in the Information shall remain at all times the property of GreenSpec and you shall acquire no rights in any such material except as expressly provided in this Agreement.

2.2 You are permitted to reproduce any part or parts either alone or in conjunction with your own material for the purposes of internal use in the your office, or for inclusion in any drawings or contract documents used or intended to be used in connection with a building contract where you are contracting party, or in connection with which you are engaged by one of the contracting parties in a professional capacity.

2.3 You shall not use, sell, assign, rent, sub-license, loan, or otherwise deal in any way in the Information or any interest in it except as expressly provided herein.

3 Disclaimer

3.1 Whilst GreenSpec endeavours to ensure that the Information is correct, it is provided on an "as is" basis, without warranties of any kind, and no warranty, express or implied, is given as to accuracy, currency or completeness and GreenSpec does not accept any liability for any error or omission.  GreenSpec shall not be liable for any third party claims or losses of any nature including, but not limited to, loss of profits, direct, indirect, special or consequential damages arising from a third party's use or inability to use this Information.

3.2 All users and others must verify the contents of the Information and ensure that its application is effective to communicate what is required by them and that the Information is fit for their intended use which has not been specified by GreenSpec.

3.3 GreenSpec accepts no responsibility for the content on any internet website to which a hypertext link from this specification exists.  The links are provided "as is" with no warranty, express or implied, for the information provided within them.

4 General

4.1 If any part of this Agreement is held by a court of competent jurisdiction to be unenforceable the validity of the remainder of the Agreement will not be affected.

4.2 This Agreement is covered by the Laws of England and Wales.

______________________________________________________]

Addenda

NBS compatibility

National Building Specification (NBS) is the industry standard specification library.

GreenSpec’s Green Building Specification (GBS) is designed to complement NBS.

GreenSpec clauses are written specifically to address issues of environmental sustainability.

NBS adopts and develops the Construction Project Information Committee’s (CPIC) classification system Common Arrangement of Work Sections (CAWS) 1998 edition.

GBS adopts and develops the CPIC and NBS versions of CAWS to enable integration into NBS-based specifications.

GBS adopts NBS clause numbering to provide for easy clause assimilation.

CPIC: www.productioninformation.org/

CAWS: www.productioninformation.org/CAWS.asp

Proposed changes: www.productioninformation.org/cawsuni/topcawsuni.asp

NBS: www.thenbs.com/